## Slide 1: Graphene plasmonics: hybrid devices
A. N. Grigorenko
The University of Manchester

## Slide 2: Authors: Manchester: A. K. Geim, K. S. Novoselov, V. G. Kravets, F. Schedin, R. Jalil, L. Britnell, R. V. Gorbachev, D. Ansell, B. Thackray Cambridge: A. C. Ferrari, T. J. Echtermeyer, P. K. Jasnos, A. Lombardo, E. Lidorikis, Marseille: A. V. Kabashin
EPSRC, EC FP7 Metachem, Samsung

## Slide 3: Talk Overview
Plasmonics
Graphene
Graphene plasmonics
Graphene optics modified by plasmonic nanostructures (SERS and photodetection)
Plasmonic response modified by graphene presence (collective resonances)
Conclusions

## Slide 4: Plasmonics
Light interaction with a structured material that contains electron plasma
Plasmon resonances in the visible light!
Strong near-fields!
What Romans did for us?

## Slide 5: New properties from structuring
Hard Steel
Huge Young modulus
Soft spring
Mattress metamaterial

## Slide 6: Example: Singular optics from nanostructuring
Phys. Rev. B, 78, 205405, 2008

## Slide 7: New properties from structuring
Graphite
Graphene

## Slide 8: Graphene
Extracted in Manchester!
The strongest
The thinnest
The fastest
The impenetrable
The cheapest
The ...

## Slide 9: Graphene’s “true colors” in optics
massless
Dirac fermions
monolayer graphene
Broadband operation
Fast response
Gating using low voltage and power
Small physical signature

## Slide 10
Visualisation of Fine Structure Constant
bilayer
graphene
air
the fine structure constant observed
“with a naked eye”
 = 1/137 (2%)
white light transmittance (%)
98
100
96
50
0
25
distance (m)

5
1
2
3
4
number of layers
88
100
96
92
white light transmittance (%)

Manchester, Science ‘08
 = 3.14.. x 1/137

## Slide 11: Graphene optics – really grey – except ultraviolet
Problem – the interaction with light is relatively weak – graphene absorbs only 2.3% of visible light
V. G. Kravets et al., Phys. Rev. B 81, 155413 (2010)

## Slide 12: To add some colours to graphene: Graphene Plasmonics
Intrinsic graphene 2D plasmons
Combination of graphene with conventional plasmonic structures with idea to boost both graphene and plasmonics applications.
Reviews:
FHL Koppens, DE Chang, FJ García de Abajo, Nano Lett, 11, 3370-3377 (2011)
Nature Photonics 6, 749–758 (2012)

## Slide 13: Intrinsic graphene plasmons
Graphene plasmons are fascinating for the following other reasons:
Graphene (Dirac) plasmons can be easily manipulated by gating and structuring;
Strong localization is possible;
the Dirac‐plasmon dispersion is affected by exchange and correlation effects;
it is easy to couple Dirac plasmons to light provided that the momentum mismatch between the latter and the former is compensated by a sufficiently “sharp" object (a periodic pattern, the tip of an AFM probe, a nanoscale defect, etc);
The lifetime of Dirac plasmons is predicted to be much longer than that of plasmons in metals or semiconductors;
Other 2D plasmonic materials are now available (bilayer, trilayer, etc.);
Koppens and Basov groups

## Slide 14: Hybrid graphene/plasmonics devices
Non-linear optics – graphene as a reliable “sensor” of electromagnetic fields.
Plasmonics to help graphene – photovoltaics.
Graphene to help plasmonics – “active” and sensing plasmonics.

## Slide 15: A. Graphene as a tool to measure enhancements of electromagnetic fields
Enhancement of Raman ~30 - just!
ACS Nano 4, 5617 (2010).
Absorption enhancement
Raman enhancement

## Slide 16
Layered material fabrication - transfer procedure
place on a substrate carrying BN
remove supporting layer
remove
sacrificial
layer
develop contacts & mesa
orient graphene
facing down
place another layer of BN on top
Layer-by-Layer
Material
Engineering
REPEAT as many times as you can

## Slide 17
Graphene transfer onto plasmonic nanoarray
remove
sacrificial
layer

## Slide 18: Graphene based plasmonics – graphene on the top
Enhancement of Raman ~1000
J. Phys. Chem. C, 2012, 116 (6), pp 3882–3887

## Slide 19: Unusual conclusion
In case of graphene, SERS is described very well by electromagnetic mechanism – maybe because of the simple 2D geometry of graphene sheet!
Hence, graphene can help to quantify field enhancement in composite plasmonic structures!
Graphene could become a test object of choice for studying field amplification in plasmonics.

## Slide 20: B. Plasmonic enhancement of graphene photo-response
Graphene photo-detectors enhanced by plasmonics
Nature Communications 2, art. no.458 (2011)

## Slide 21
Working principle of graphene photovoltaics
Metal-induced doping
Giovanetti et. al., Phys. Rev. Lett. 101, 026803 (2008).
e-h pair creation
Metal
e-h separation

## Slide 22
Contacts
Marry Graphene & Plasmonics
Photovoltage, 633nm
Enhancement : x20
Can be illuminated by flood light
Graphene Photovoltaics

## Slide 23: Graphene-plasmonic photocells
(a)-(f) Wavelength dependence 457nm-785nm

## Slide 24: Details of photoconversion
Not clear yet!
thermoelectric effects have been demonstrated in direct measurements of the symmetry of six‐fold photovoltage patterns as a function of bottom‐ and topgate voltages: at low temperatures nonlocal hot carrier transport dominates the intrinsic photoresponse in plain graphene with non‐structured electrodes
Gabor et al. Science 334, 648 (2011).

## Slide 25: Another open question - resistive coupling of plasmonic resonances
Graphene allows resistive coupling of plasmonic resonances – active plasmonics?
E
+
-
+
-
+
-
+
-
E
j

## Slide 26: Nanoparticles on a conducting sub-layer
Nature Communications, vol. 3, 640, 2012.
No sublayer
5nm Ti sublayer
5nm Cr sublayer

## Slide 27
Nanoparticles on a conducting sub-layer
Nature Communications, vol. 3, 640, 2012.
Size dependence
Ambient medium

## Slide 28: Graphene Photovoltaics – future directions
Vertical geometry – Novoselov et al.
Other 2D materials for charge separation.
Optimization of plasmonic elements.
Broadband emitters.

## Slide 29: C. Graphene to help plasmonics
Holy Grail: active graphene based plasmonics (small, cheap, fast, low power consumption, etc.)
Problems:
Gating difficult to arrange (to much metal around)
Graphene doping by metal.
Graphene ripples, bubbles, etc.

## Slide 30: Example: graphene affecting optical properties of plasmonic elements
Diffractive coupled plasmonic resonances = aka geometric resonances = aka collective plasmon resonances
0-order
-1
1
2
When a diffracted mode becomes grazing – it sees a lot of gold – should demonstrate strong absorption (Wood, Rayleigh, Markel, Schatz)

## Slide 31: Diffractive coupled resonances
Phys. Rev. Lett., vol. 101, 087403, 2008.

## Slide 32: Diffractive coupled resonances can result in huge phase sensitivity!
Opt. Lett. 35, 956 (2010)
Optics Express, vol. 17, No. 23, 21191-21204, 2009.

## Slide 33: Darkness = phase sensitivity!
Appl. Phys. Lett. 75, 3917 (1999)

## Slide 34: Huge phase sensitivity is connected to singular optics
Nye, J. F. & Berry, M. V., Dislocations in Wave Trains. Proceedings of the Royal Society of London. A. Mathematical and Physical Sciences 336, 165-190 (1974)
E=0 phase is not defined!
Phase is atan(y/x)

## Slide 35: Singular Optics
Photons with J>1 – Requires E=0 – points (lines) of darkness

## Slide 36: Singular Optics – Topological Darkness from structured metal
Reflection=0
a
b
Natural materials do not like this region
Nature Materials (2013) doi:10.1038/nmat3537

## Slide 37: Singular Optics – Topological Darkness
Ag

## Slide 38: Topological Darkness
Exists even for extremely thin subwavelength layers.
The point of zero reflection is topologically protected owing to the Jordan curve theorem.
Topologically stable under small imperfections in structure.

## Slide 39
Use transfer procedure to create hybrid devices
remove
sacrificial
layer

## Slide 40: Graphene modified plasmonics
J. Phys. Chem. C, 2012, 116 (6), pp 3882–3887

## Slide 41: Graphene modified plasmonics - surface chemistry of graphene
To modify graphene properties we used graphene hydrogenation by atomic H produced by hydrogen plasma exposure.
Hydrogenation changes graphene conductivity and dielectric constants
Hydrogenation can be monitored using Raman

## Slide 42: Graphene hydrogenation studied by collective resonances
J. Phys. Chem. C, 2012, 116 (6), pp 3882–3887

## Slide 43: Graphene hydrogenation
1% hydrogenation
mass density of <1 pg/mm2
was detected!
the areal mass phase sensitivity could be better than 0.1 fg/mm2
This corresponds to just ~10 H atoms per one nanodot!
Nature Materials (2013) doi:10.1038/nmat3537

## Slide 44: Sensitivity comparison
Localized plasmons – areal sensitivity 1000 pg/mm2
Surface Plasmon Resonance – areal sensitivity 1 pg/mm2
Phase sensitive nano-optics – areal sensitivity 0.1 fg/mm2
Due to the well defined 2D geometry and possibility to monitor hydrogenation ratio using Raman, graphene could become a test object of choice for studying areal mass sensitivity in plasmonic nano-sensors!

## Slide 45: Biosensing
Streptavidin
Biotin
Nature Materials (2013) doi:10.1038/nmat3537

## Slide 46: Biosensing - sensitivity
Experimental sensitivity of 1-4 molecules per nanodot. We used Biotin-Streptavidin pair with the size of detected Streptavidin 60 kDa – Hydrogen is just 1 Da, for comparison.
Sensitivity limit for biosensing: attachment of 1 Streptavidin molecule per ~300 nanodots (areal sensitivity of 1 fg/mm2)
We are close to single molecule detection using optical transduction!

## Slide 47: Conclusion
Graphene plasmonics is not that grey!
Graphene can benefit from plasmonic nanostructures - SERS and photodetection.
Graphene can be a test object for measuring electromagnetic field enhancement in plasmonic nanostructures .
Graphene chemistry can be used to calibrate plasmonic nanosensors.
Future of hybrid graphene/plasmonics devices : vertical geometry, graphene derivatives, active optical elements.
Thank you for your attention!