## Slide 1: 1. Confinement-Induced Loss – Penultimate Limit in Plasmonics 2. Demystifying Hyperbolic Metamaterials using Kronig Penney Approach
Jacob B Khurgin
Johns Hopkins University, Baltimore –MD

## Slide 2: Confinement (a.k.a.) surface absorption of SPP in metals
EF
E
k
k
k~w/vF
If the SPP has the same wave vector kp=k~w/vF Landau damping takes place
Since kp =w/vP the phase velocity of SPP should be equal to Fermi velocity or about c/250….
For visible light leff ~l0/250~2nm –too small
wmet
wd
ed>0
em<0
But due to small penetration length there will be Fourier component with a proper wave-vector – absorption will take place

## Slide 3
q
EF
E(x)
Confinement (a.k.a.) surface absorption of SPP in metals
One can think of this as effect of momentum conservation violation due to reflection of electrons from the SMOOTH surface

## Slide 4: Phenomenological Interpretation
In frequency space the resonance shifts from 0 to
Integration over Lindhard function gives the same result
Lindhard Formula
er(K)
Dw
er
w
er(0)
In K-space – two peaks at
-1.5K0
-K0
-0.5K0
0
0.5K0
K0
1.5K0
-10
-5
0
5
10
15
20
25
Wavevector K
Arbitrary units
2q

## Slide 5: Influence of nano-confinement on dispersion
Ag*
Au*
Ag
Au
Ideal
0
100
200
300
400
30
32
34
36
38
Wave vector in dielectric (mm-1)
SPP wave vector (mm-1)
Light line in dielectric
wmet
wd
ed~5
AlGaN
lspp~345nm
Ag* g=3.2×1013 s-1
no confinement effect
Ag g=3.2×1013 s-1
with confinement effect
Au* g=1×1014 s-1
no confinement effect
Au g=1×1014 s-1
with confinement effect
Ideal g=0 s-1
with confinement effect
Confinement (surface) scattering is the dominant factor!

## Slide 6
10
-3
10
-2
10
-1
10
-2
10
0
10
2
Ag*
Au*
Ag
Au
Ideal
Effective width (mm)
Propagation Length (mm)
Influence of nano-confinement on loss
wmet
wd
ed~5
AlGaN
lspp~345nm
Confinement (surface) scattering is the dominant factor !
Close to SPP resonance los sdoes not depend on Q of metal itself! !

## Slide 7
Ag*
Ag
Au*
Au
Ideal
Influence of nano-confinement on loss of gap SPP
10
-2
10
-1
10
-1
10
0
10
1
10
2
Effective width (mm)
Propagation Length (mm)
wmet
w
ed~12
InGaAsP
lspp~1550nm
Dispersion is the same for all metals
Surface-induced absorption dominates for narrow gaps

## Slide 8: For more involved shapes
Field concentration is achieved when higher order modes that are small and have small (or 0) dipole and hence normally dark gets coupled to the dipole modes of the second particle. But, due to the surface (Kreibig, confinement) contribution the smaller is the mode the lossier it gets and hence it couples less. One can think about it as diffusion-main nonlocal effect!
PHYSICAL REVIEW B 84, 045415 (2011)

## Slide 9: Conclusions 1
Presence of high K-vector components in the confined field increases damping and prevents further concentration and enhancement of fields…
For as long as there exists a final state for the electron to make a transition…it probably will
The effect of damping of the high K-components is equivalent to the diffusion

## Slide 10: 2. Demystifying Hyperbolic metamaterials – Kronig Penney approach
Gaudi, Sagrada Familia

## Slide 11: Hyperbolic Dispersion
Jacob, Z., Alekseyev, L. V. & Narimanov, E. Optical hyperlens: far-field imaging beyond the diffraction limit. Opt. Express 14, 8247–8256 (2006).
Salandrino, A. & Engheta, N. Far-field subdiffraction optical microscopy using metamaterial crystals: theory and simulations. Phys. Rev. B 74, 075103 (2006).
kx
ky
kz
kx
ky
kz
kx
ky
kz
Elliptical k-limited
Hypebolic k-unlimited

## Slide 12: Hyperbolic materials and their promise
High k implies high resolution
– beating diffraction limit -hyperlens
High k implies large density of states – Purcell Effect
If ei~0 ENZ material
Problems: negative e is usually associated with high loss

## Slide 13: Natural Hyperbolic Materials
Natural hyperbolic materials: CaCO3, hBN, Bi – phonon resonances in mid-IR
(also plasma in ionosphere –microwaves)

## Slide 14: Hyperbolic Metamaterials (effective medium theory)
X
Y
Z
em<0
ed>0
b
a
kx
ky
kz
kx
ky
kz

## Slide 15: Granularity
em<0
ed>0
b
a
When effective wavelength becomes comparable to the period – k~p/(a+b) non locality sets in and effective medium approach fails (Mortensen et al, Nature Comm 2014), Jacob et al (2013) (Kivshar’s group).
Alternatively, according to Bloch theorem p/(a+b) is the Brillouin zone boundary and thus defines maximum wavevector in x or y direction. (Sipe et al, Phys Rev A (2013)B

## Slide 16: Gap and slab plasmons (a.k.a. transmission lines)
em<0
ed>0
b
a
Gap SPP
Slab SPP
There must be a relation.
So, what happens in hyperbolic material that makes it different from coupled SPP modes?

## Slide 17: When does the transition occur and magic happen?
Here?
or maybe here?

## Slide 18: Kronig Penney Model
Lord W. G. Penney

## Slide 19: Set Up Equations
0
a
a+b
-b
Hy
Ez
Ex
Periodic boundary conditions
Characteristic Equation

## Slide 20: Wave surfaces for different filling ratios
l=520 nm Ag em=-11+0.3i Al203 ed=1.82
a=15nm
b=15nm
ez=8.6 ex,y= -3.4
kz (mm-1)
kx (mm-1)
Effective medium works for small k’s
Effective medium
K-P

## Slide 21: Wave surfaces for different filling ratios
l=520 nm Ag em=-11+0.3i Al203 ed=1.82
a=18nm
b=12nm
ez=6.4 ex,y= -2.5
kz (mm-1)
kx (mm-1)
Effective medium works for small k’s
Effective medium
K-P

## Slide 22: Wave surfaces for different filling ratios
l=520 nm Ag em=-11+0.3i Al203 ed=1.82
a=21nm
b=9nm
ez=5.0 ex,y= -1.13
kz (mm-1)
kx (mm-1)
Effective medium works for small k’s
Effective medium
K-P

## Slide 23: Wave surfaces for different filling ratios
l=520 nm Ag em=-11+0.3i Al203 ed=1.82
a=23.4nm
b=6.6 nm
ez= 4.31 ex,y= -0.003
kz (mm-1)
kx (mm-1)
Effective medium theory predicts
ENZ negative material – but we observe both elliptical and hyperbolic dispersions
Effective medium
K-P

## Slide 24: Wave surfaces for different filling ratios
l=520 nm Ag em=-11+0.3i Al203 ed=1.82
a=23.7nm
b=6.3 nm
ez= 4.23 ex,y= 0.13
kz (mm-1)
kx (mm-1)
Effective medium theory predicts
ENZ positive material – but we observe both elliptical and hyperbolic dispersions
Effective medium
K-P

## Slide 25: Wave surfaces for different filling ratios
l=520 nm Ag em=-11+0.3i Al203 ed=1.82
a=27nm
b=3 nm
ez= 3.6 ex,y= 1.7
kz (mm-1)
kx (mm-1)
Effective medium theory predicts elliptical dispersion
But in reality there is always a region with hyperbolic dispersion at large kx – coupled SPP’s?
Effective medium and K-P
K-P

## Slide 26: Effect of changing filling ratios form 10:1 to 1:1
0
20
40
60
80
100
0
50
100
150
200
l=520 nm Ag em=-11+0.3i Al203 ed=1.82
a+b=30nm
kz (mm-1)
kx (mm-1)
Notice: hyperbolic region is always there!

## Slide 27: Effect of granularity
l=520 nm Ag em=-11+0.3i Al203 ed=1.82
a:b=7:3
kz (mm-1)
kx (mm-1)
For small period elliptical region disappears and the curve approaches the effective medium

## Slide 28: Explore the fields at different points
Fields:
Energy density:
Effective impedance:
Poynting vector
Fraction of Energy in the metal:
Effective loss:
Group velocity
Propagation length:

## Slide 29: Near kx=0
Hy
Ez
Ex
UM
UE
SZ
Sx
Magnetic Field
Energy Density
Electric Field
Poynting Vector
Vg=0.70Vd
h=1.12hd
f=.22
t=54 fs
L=6.5 mm
|E|/hd~|H|
Sign Change
In metal

## Slide 30: Near kx=kmax/2
Hy
Ez
Ex
UM
UE
SZ
Sx
Magnetic Field
Energy Density
Electric Field
Poynting Vector
|E|/hd>|H|
Sign Change
In metal –S small
Vg=0.22Vd
h=3.25hd
f=.56
t=21fs
L=0.83mm
More energy in metal
Less magnetic field

## Slide 31: Near kx=kmax
Hy
Ez
Ex
UM
UE
SZ
Sx
Magnetic Field-small
Energy Density
Electric Field
Poynting Vector
|E|/hd>>|H|
Sign Change
In metal –S small
More than half of energy in metal
Vg=0.17Vd
h=3.78hd
f=.57
t=20fs
L=0.64mm
E-field is nearly normal to wave surface –longitudinal wave!

## Slide 32: Density of states and Purcell Factor
1.5
2
2.5
3
3.5
4
4.5
5
0
5
10
15
20
Spatial Frequency (relative to kd)
Density of states
1.5
2
2.5
3
3.5
4
4.5
5
1
2
3
4
5
6
Spatial Frequency (relative to kd)
Slow down factor and impedance
n/Vg
h
Lifetime (fs)
Propagation Length (mm)
1.5
2
2.5
3
3.5
4
4.5
5
10
-1
10
0
10
1
10
2
t=1/geff
L
Purcell Factor=22
However, most of the emission is into lossy waves that do not propagate well and in addition they get reflected at the boundary
This is quenching!

## Slide 33: A Better Structure?
Purcell Factor=200!
But…it looks simply as a set of decoupled slab SPP’s
UM~0
UE
This wave does not propagate
Vg=0.055 Vd
h=6.34 hd
f=.68
t=20fs
L=0.18 mm
l=400 nm
a=12nm
b=8nm
UM
kz (mm-1)
kx (mm-1)
Virtually no magnetic field – hence a tiny Poynting vector
With half of energy inside the metal
Metamaterial that aspires to be ENZ

## Slide 34: Assessment
The states with high density and large spatial frequency
have propagation length of about 100-200nm
So, all we can see is quenching
This is no wonder – new states are not pulled out of the magic hat – they are simply the electronic degrees of freedom coupled to photon…and they are lossy
n/Vg
h
0
1
2
3
4
5
6
7
8
0
5
10
15
20
25
30
35
Spatial Frequency (rel. to kd)
Slow Down and Impedance (rel.unit)
0
1
2
3
4
5
6
7
8
0
20
40
60
80
100
Density of states
Spatial Frequency (rel. to kd)
t=1/geff
L
0
1
2
3
4
5
6
7
8
10
-1
10
0
10
1
10
Lifetime in fs and Propagation in mcm
2
Spatial Frequency (rel. to kd)

## Slide 35: In plane dispersion 1200-400 nm
It looks exactly as gap SPP or slab SPP
UM
kz (mm-1)
kx (mm-1)
0
50
100
150
0
50
100
150
200
250

## Slide 36: Normal to the plane dispersion 1200-400 nm
It looks exactly as coupled waveguides should look….or as conduction and valence bands
UM
kz (mm-1)
kx (mm-1)
0
50
100
150
0
50
100
150
200
250

## Slide 37: Parallels with the solid state
The wave function of electron in the band is
For transport properties we often ”homogenize” the wave function by introducing the effective mass
But to understand most of the properties one must the consider periodic part of Bloch function
Similarly, for metamaterials, effective dielectric constant gives us a very limited amount of information – we must always look at local field distribution, especially because it is so damn easy.

## Slide 38: Conclusions
Hyperbolic metamaterials are indeed nothing but coupled slab (or gap) SPP’s. If it looks like a duck, walks like a duck, and quacks like a duck, it is probably a duck. Why use more than 3 layers is unclear to me
The Purcell factor is no different from the one near simple metal surface – most of radiation goes into the slowly propagating (low vg) and lossy(short L) modes that do not couple well to the outside world (high impedance). There are easier ways of modifying PL
In general, outside the realm of magic, new quantum states cannot appear out of nowhere – states are degrees of freedom. Density of photon states can only be enhanced by coupling with electronic (ionic) degrees of freedom (of which there are plenty) That makes coupled modes slow and dissipating heavily. There is no way around it unless one can find materials with lower loss.
In general, Bloch (Foucquet) theorem states that if one has a periodic structure with period d, one may always find a solution
F(x)=u(x)ejkx where u(x) is a periodic function with the same period. But it does not really mean that one has a propagating wave if the group velocity is close to zero.
It is important to analyze the periodic “tight binding” function u(x) and Kronig Penney method is a nice and simple tool for it