## Slide 1
Outline
Damping mechanisms
l Plasmons in ribbons
Experimental results
Graphene Nanophotonics
Benasque, 2013, Mar 03 -- Mar 08
Momentum dependence and losses in graphene plasmons
Mid-infrared plasmons in scaled graphene nanostructures
H. Yan, T. Low, W. Zhu, Y. Wu, M. Freitag, X. Li, F. G., P. Avouris, F. Xia
arXiv:1209.1984, Nature Photonics, in press
L. Martín-Moreno, A. Nikitin, F. García-Vidal, M. M. Fogler

## Slide 2
Damping mechanisms
l Higher order processes, multiple electron-hole pairs
Lack of momentum conservation
l Decay into other excitations: phonons, …

## Slide 3
Elastic scattering
elastic mean free path
k+q
k
k’

## Slide 4
D
Finite systems

## Slide 5
Inhomogeneous electric fields
Edges
Local excitations
wp(q) 4 q 4 L-1
T. Low, M. M. Fogler, F. G, unpublished

## Slide 6
Inhomogeneous electric fields
t=1ms, E =0.4eV
F
Non local conductivity, clean system

## Slide 7
Surface polar modes
Si O has polar modes which induce long range electrostatic potentials. The dielectric constant of the system is modified.
2

## Slide 8
Optical phonons
Optical phonons at G, w =0.2 eV
ph
Coupling through changes in bond lengths
Weak dispersion
1/t
e
k
k+q
q
k’

## Slide 9
Experiments
Nanoribbons, antidots , and nanodisks defined by electron beam litography.
The samples lie on CVD graphene on SiO and diamond like carbon (DLC) substrates.
2
Y. Yan, T. Low, W. Zhu,Y. Wu, M. Freitag, X. Li, F. G., P. Avouris, and F. Xia, arXiv:1209.1984, Nature Phys., in press

## Slide 10
Plasmon dispersion
dead layer
asymmetric lineshape
graphene on diamond like carbon (DLC)

## Slide 11
Plasmon dispersion
graphene on SiO
2

## Slide 12
Plasmon damping

## Slide 13
Plasmon damping
Comparison between graphene on SiO and graphene on DLC
2
Doping dependence

## Slide 14
Conclusions. Open questions
l Plasmon dispersion can be accurately measured in nanoribbons.
Plasmon linewidth can be explained by simple mechanisms
The main decay channel at high frequencies is decay into optical phonons and electron-hole pairs
The role of other decay channels is in reasonable agreement with simple estimates
l Coulomb blockade, interplay between plasmons and dc transport