## Slide 1
Boosting local field enhancement
by on-chip nanofocusing and impedance-matched plasmonic antennas
Vladimir A. Zenin, Ilya P. Radko, Valentyn S. Volkov and Sergey I. Bozhevolnyi Centre for Nano Optics, University of Southern Denmark, Campusvej 55, 5230 Odense M, Denmark zenin@iti.sdu.dk
Andrei Andryieuski, Radu Malureanu and Andrei V. Lavrinenko DTU Fotonik, Technical University of Denmark, Oersteds pl. 343, 2800 Kongens Lyngby, Denmark
Dmitri K. Gramotnev Nanophotonics Pty. Ltd., GPO Box 786, Albany Creek, Queensland 4035, Australia.
Nanolight 2016, Benasque

## Slide 2
Theoretical principles of adiabatic nanofocusing

## Slide 3
Focusing of gap-SPP

## Slide 4
Focusing of SPP along metal cone

## Slide 5
Focusing of SPP along metal strip

## Slide 6
Nanofocusing with constant adiabatic parameter
λ = 1500 nm
γ = 0.015
-p
p
0
max
0
1 μm
Amplitude
Phase
Ohmic losses should be taken into account!
nSilica
w = 30 nm
w = 1.5 μm

## Slide 7
Optimization of the combined taper
L1
L2
1500 nm
150 nm
30 nm
Andrei Andryieuski
For optimum parameters:
Transmittance Ttotal ≈ 40%
Total FE ≈ 12

## Slide 8
Silica
Transmission-mode s-SNOM
Towards detector
AFM tip

## Slide 9
Transmission-mode s-SNOM
Demodulation
Detector
Polarizer
Beam splitter
Beam splitter
Telecom laser
1425-1640 nm
Oscillating mirror
Parabolic mirror
Parabolic mirror
Amplitude |E|
Phase f
AFM tip

## Slide 10
2 µm
Topo
|E|
Arg[E]
|E|
Arg[E]
|E|
Arg[E]
|E|
Arg[E]
30 nm
60 nm
100 nm
200 nm
Nanofocusing to strip waveguides
2 µm
Radu Malureanu

## Slide 11
100 nm
Discrete Fourier Transform (log scale)
x
kz
1.6k0
-1.6k0
Global fitting parameters (complex): n, r
+
=
|E|
10|E|
Re[n] = 1.60
Lprop = 4.5 μm
R = |r|2 = 0.10
Processing data
|E|
|E|
Arg[E]

## Slide 12
Fitting with two modes

## Slide 13
Strip waveguide properties
Mode profile
Mode dispersion
V. A. Zenin, R. Malureanu, I. P. Radko, A. V. Lavrinenko, and S. I. Bozhevolnyi, “Near-field characterization of bound plasmonic modes in metal strip waveguides,” Opt. Express, 24(5), 4582-4590 (2016).

## Slide 14
Estimation of the transmittance
Tout
Rout
In
Rin
x
z
1.5 µm
Fit
Ttotal ≈ 20%
Tsingle ≈ 81%
Ttotal ≈ 31%
Tsingle ≈ 56%

## Slide 15
Further increase in FE: gap in the nanowire
E1
E2
Boundary conditions:
ε1E1 = ε2E2
E2 = E1ε1/ε2
For 10 nm gap longitudinal FE ~ 22; FE = 22/3.8 ≈ 6.

## Slide 16
Further increase in FE: antenna excitation
Antenna-coupled nanowire
Antenna-coupled nanofocuser
For 10 nm gap at resonant antenna length (240 nm) total FE ≈ 9.
|E|
100 nm

## Slide 17
Experimental comparison
TSNF
t-TSNF
a-TSNF
V. A. Zenin, A. Andryieuski, R. Malureanu, I. P. Radko, V. S. Volkov, D. K. Gramotnev, A. V. Lavrinenko, and S. I. Bozhevolnyi, “Boosting local field enhancement by on-chip nanofocusing and impedance-matched plasmonic antennas,” Nano Lett. 15, 8148-8154 (2015).

## Slide 18
Conclusions
Dispersion properties of strip waveguides (w = 30, 60, 100, 200, 500, and 1500 nm) are investigated
Optimized 2-section taper with transmittance T > 40% (sim. + exp.) results in the FE of ~12 (intensity enhancement of ~140)
Resonantly coupled antenna further boosts intensity enhancement up to ~12000, with the enhanced field being evenly distributed over the gap volume of 30×30×10 nm3
Thank you!