## Slide 1
Approximations to the exchange-correlation functional

## Slide 2
Local density approximation (LDA)
Result: lattice constants and bonding distances much too large (20%-50%)
LDA (Kohn and Sham, 1965)
xc energy per particle of a uniform electron gas of density ρ
(known from quantum Monte-Carlo and many-body theory)
Result: decent lattice constants, phonons, surface energies of metals

## Slide 3
Quantity | Typical deviation (from expt) | 
Atomic & molecular ground state energies |  | < 0.5 %
Molecular equilibrium distances |  | < 5 %
Band structure of metals, Fermi surfaces |  | few %
Lattice constants |  | < 2 %

## Slide 4
Quantity | Typical deviation (from expt) | 
Atomic & molecular ground state energies |  | < 0.5 %
Molecular equilibrium distances |  | < 5 %
Band structure of metals, Fermi surfaces |  | few %
Lattice constants |  | < 2 %
Systematic error of LDA: Molecular atomisation energies too large and bond lengths
and lattice constants too small

## Slide 5
One would expect the LDA to be good only for weakly
inhomogeneous systems, i.e., systems whose density satisfies:
and
Why is the LDA good also for strongly inhomogeneous systems?
Answer: Satisfaction of many exact constraints (features of exact xc fctl)
coupling-constant-averaged xc hole density
Important constraints:
are satisfied in LDA

## Slide 6
Generalized Gradient Approximations (GGA)
Langreth, Mehl (1983), Becke (1986), Perdew, Wang (1988)
PBE: Perdew, Burke, Ernzerhof (1996)
Construction principle: Satisfaction of exact constraints
(important lesson from LDA and from gradient expansion of Exc )
Results: GGAs reduce the LDA error in the atomisation energy
significantly (but not completely) while LDA bond lengths are
over-corrected (i.e. are in GGA too large compared with expt)

## Slide 7
Detailed study of molecules (atomization energies)
32 molecules (all neutral diatomics from first-row atoms only and H2 )
B. G. Johnson, P. M. W. Gill, J. A. Pople, J. Chem. Phys. 97, 7847 (1992)
Atomization energies (kcal/mol) from:
mean deviation from experiment 0.1 1.0 -85.8
mean absolute deviation 4.4 5.6 85.8
for comparison: MP2
-22.4
22.4

## Slide 8
LIMITATIONS OF LDA/GGA
Not free from spurious self-interactions: KS potential decays more rapidly than r-1 for finite systems
Consequences: – no Rydberg series
– negative atomic ions not bound
– ionization potentials (if calculated from highest occupied orbital energy) too small
Dispersion forces cannot be described
Wint (R) e-R (rather than R-6)
band gaps too small: G
Egap (LDA/GGA) ≈ 0.5 Egap(expt)
Energy-structure dilemma of GGAs
atomisation energies too large
bond lengths too large
(no GGA known that gets both correct!!)
Wrong ground state for strongly correlated solids, e.g. CoO, La2CuO4 predicted as metals

## Slide 9
Meta Generalized Gradient Approximations (MGGA)
Result: Solves energy-structure dilemma of GGAs

## Slide 10
LDA
GGA
MGGA
hybrid
occupied orbitals (e.g. fraction of EXX)
RPA-like
occupied & unoccupied KS orbitals + energies
earth
(Hartree )
heaven
(exact functional)
Jacob’s ladder of xc functionals (John Perdew)

## Slide 11
DFT description of quantum phases:
Magnetism and
Superconductivity

## Slide 12
MAGNETIC SYSTEMS
In principle, Hohenberg-Kohn theorem guarantees that m(r) is a
functional of the density: m(r) = m[ρ](r). In practice, good
approximations for the functional m[ρ] are not known.
Quantity of interest: Spin magnetization density m(r)
Include m(r) as basic variable in the formalism, in addition
to the density ρ(r).

## Slide 13
HK theorem
total energy:
universal
Start from fully interacting Hamiltonian with Zeeman term:

## Slide 14
KS scheme
For simplicity:
,
vxc[,m] = Exc[,m]/ 
Bxc[,m] = Exc[,m]/ m
 (r) = + (r) + - (r) ,
m (r) = + (r) - - (r) ,
± =  j± 2
B  0 limit
These equations do not reduce to the original KS equations for B  0 if, in this limit, the system has a finite m(r).
vxc(r)
Bxc(r)

## Slide 15
DENSITY-FUNTIONAL THEORY OF THE SUPERCONDUCTING STATE
Include order parameter, χ , characterising
superconductivity as additional “density”
BASIC IDEA:
L.N. Oliveira, E.K.U.G., W. Kohn, PRL 60, 2430 (1988)
Include N-body density, Γ, of the nuclei as additional “density”
T. Kreibich, E.K.U.G., PRL 86, 2984 (2001)

## Slide 16
General (model-independent) characterization of superconductors:
Off-diagonal long-range order of the 2-body density matrix:
order parameter of the N-S phase transition

## Slide 17
Hamiltonian

## Slide 18
S
N

F
P
B

x
x
m
ANALOGY
“proximity effect”

## Slide 19
Hamiltonian
3 densities:
electron density
order parameter
diagonal of nuclear Nn-body density matrix

## Slide 20
Hohenberg-Kohn theorem for superconductors
Densities in thermal equilibrium
at finite temperature
[v(r),(r,r’),W(R)]  [(r),(r,r’),(R)]
1-1

## Slide 21
Electronic KS equation
vs[,,](r)
s[,,](r,r’)
vs[,,](r)
s*[,,](r,r’)
Nuclear KS equation
Ws[,,](R)
3 KS potentials:
vs s Ws
KS theorem:
There exist functionals vs[,,], s[,,], Ws[,,], such that the above equations reproduce the exact densities of the interacting system
No approximation yet!
“Exactification” of BdG mean-field eqs.

## Slide 22
Electronic KS equation
vs[,,](r)
s[,,](r,r’)
vs[,,](r)
s*[,,](r,r’)
Nuclear KS equation
Ws[,,](R)
3 KS potentials:
vs s Ws
KS theorem:
There exist functionals vs[,,], s[,,], Ws[,,], such that the above equations reproduce the exact densities of the interacting system
No approximation yet!
“Exactification” of BdG mean-field eqs.
Solved in harmonic approximation

## Slide 23
CONSTRUCTION OF APPROXIMATE Fxc :
develop diagrammatic many-body perturbation theory on the basis of the Ho-propagators:
Gs normal electron propagator (in superconducting state)
Fs
Fs*
Ds phonon propagator
Immediate consequence:
Fxc = Fxc + Fxc
all diagrams containing Ds
all others diagrams
ph
el
anomalous electron propagators

## Slide 24
Phononic contributions
First order in phonon propagator:
Calculated with Quantum Espresso code
Fxc
ph
Input to
: Full k,k’
resolved Eliashberg function

## Slide 25
Purely electronic contributions
RPA-screened electron-electron interaction
]
ρ
[
F
,
ρ
F
GGA
xc
ee
xc
+
=
c
Crucial point: NO ADJUSTABLE PARAMETERS
[ ]

## Slide 26
Full Green fctn
KS Green fctn

## Slide 27
Ab-initio calculation of SC order parameter χ(r,r’) for MgB2
χ(r,r’) ≡ χ(R,s)
R = (r+r’)/2
s = r-r’
s = 0
s = (0,0, 0.5)
s = (10,0,0)
s = (0,0, 1.5)
χ(R,s) as function of R
for fixed s.

## Slide 28
MgB2
χ(R, s=0) as function of R
A. Linscheid, A. Sanna, E. K. U. Gross, Phys. Rev. Lett. 115, 097002 (2015).

## Slide 29
C2H2
χ(R0,s) as function of s (R0 fixed at middle of C-C σ bond)

## Slide 30
Pb monolayer on Si
χ(R, s=0)

## Slide 31
Pb monolayer on Si
χ(R, s=0)
superconducting
metallic band of Si