## Slide 1: Plasmonic antenna platforms for multicolor single-molecule studies with high-throughput
Ediz Herkert
Prof. María F. García-Parajo
Single Molecule Biophotonics
Nanolight 2022

## Slide 2: How to detect single molecules?
Notes: Coarse categorization in far-field and near-field methods
Far field: source far away from specimen -> diffraction limit
Near field: source close to speciment (sub-wvl) -> no diffraction limit
I contrast to that nanoantenna provide directly sub-diffraction illumination volume

## Slide 3: Why nanoantennas for life sciences?
Field-confinement
Field-enhancement
LDOS modification
Holzmeister et al., Chem. Soc. Rev., 43, 1014-1028 (2014)
Anger et al., Phys. Rev. Lett, 96, 3-6 (2006)
Notes: Why are nanoantennas important?
Diffraction limit prohibits to observe bio-interactions
Nanoantennas provide to access this regine and offer three advantages
Fermi‘s golden rule + purcell effect

## Slide 4: What are challenges in fluorescence experiments with nanoantennas?
Broadband resonance of Al-bowtie arrays
Multiplexed multicolor excitation
Fluorescent background
Chemical interactions between molecules & metal
Al-aperture
Ultrathin Al2O3 passivation layer (~3 nm)
EBL-based Al-Antenna-in-Box (Al-AiB)
Notes: Explanation of AiB
~10,000 antennas

## Slide 5: How to fabricate Al-AiBs?
Flauraud et al., Nano Lett., 17, 1703-1710 (2017)

## Slide 6: How to design multicolor AiBs?
Notes: This means that the bowtie length and aperture diameter are the parameter to optimize
FDTD simulations show gain in intensity enhancement as function of the aperture diameter
Dashed line indicates modes of empty aperture
Red line is the optimal aperture choice for given length
2x more intensity-enhancement & tunability over full VIS
Not only background suppression but also intensity enhancement
In regard to the fabrication the sensitivity of the IE to displacement is important
Displacement up to 50nm can be accepted

## Slide 7: How accurately can we fabricate Al-AiBs?
Notes: Difficulty of design that process based on negative resist is preferable but offered resolution is too low
Combination of negative and positive resist with intra-writefield alignment yielded best results
Process allows to fabricate large-area structures with previously identified requirements
Objective can be considered finished as biocompatibility will only become important for last objective

## Slide 8: How to confirm multicolor fluorescence enhancement of Al-AiBs?
Notes: Preliminary experiments with simple bowties and immobilized AF647 carried out
Same power used
Hint for higher photostability
Two types of experiments w. bowties & AiBs to demonstrate advantages

## Slide 9: What is the multicolor fluorescence enhancement of Al-apertures?

## Slide 10: What is the multicolor fluorescence enhancement of Al-apertures?

## Slide 11: What is the multicolor fluorescence enhancement of Al-apertures?
Instrument response function:
Multiexponential decay:

## Slide 12: What is the multicolor fluorescence enhancement of Al-apertures?

## Slide 13: What did we learn and where do we go next?
Optimization
Background reduction & stronger broadband excitation
3-step EBL process
Fabrication of ~10,000 Al-AiBs w. required geometrical parameters
For Al-apertures:
Fluorescence reduction
Metal induced quenching
Fabrication
Validation
(Ongoing)
Widefield excitation
sCMOS readout
Multiplexing (Outlook)

## Slide 14
Pamina Winkler
Single Molecule Biophotonics
This project has received funding from the European Union’s Horizon 2020 research and innovation program under the Marie Sklodowska-Curie grant agreement No 812992.
Maria Sanz-Paz